## Slide 1: Evaluating the ASR Potential of Aggregates and Effectiveness of ASR Mitigation Measures in Miniature Concrete Prism Test
Enamur R Latifee, Graduate Student
Glenn Department of Civil Engineering
Clemson University
Concrete Materials Seminar
February 17, 2012

## Slide 2: Acknowledgement
Dr. Prasad Rangaraju,
Associate Professor,
Glenn Department of Civil Engineering Clemson University
Dr. Paul Virmani, FHWA

## Slide 3: Presentation Outline
ASR review
Introduction to Miniature Concrete Prism Test (MCPT)
Evaluation of Effectiveness of SCMs for ASR Mitigation in the MCPT
Effect of Prolonged Curing of Test Specimens on the Performance of Fly Ashes in MCPT Test Method

## Slide 4: Beginning of ASR Research

## Slide 7: Alkali-Silica Reaction Distresses in the field
Notes: Delete

## Slide 8: Field symptoms of ASR in concrete structures

## Slide 9: More ASR Distress

## Slide 10: Some Case Histories
Buck Hydroelectric plant on New River (Virginia, US)
Arch dam in California
  crown deflection of 127 mm in 9 years
Railroad Canyon Dam
Morrow Point Dam, Colorado, USA
Stewart Mountain Dam, Arizona
Parker Dam (Arizona)
  expansion in excess of 0.1 percent

## Slide 11
Hydroelectric dam built in 1938
180 mm of arch deflection due to alkali silica gel expansion
Cracking and gel flow in concrete
Case Study: Parker Dam, California
http://www.acres.com/aar/
Alkali-Aggregate Reactions in Hydroelectric Plants and Dams:

## Slide 12
Possible ASR damage on concrete retaining wall
Case Study: I-85 - Atlanta, Georgia

## Slide 13
Typical Distress Observed in Concrete Pavement Exposed to Airfield Deicing Chemicals

## Slide 14
Typical Distress Observed in Concrete Pavement Exposed to Airfield Deicing Chemicals

## Slide 15
Example: Shek Wu Hui Treatment plant, Hong Kong

## Slide 16
Example: Daqing Railway Bridge, China

## Slide 17
Countries reported ASR problems
1 | AUSTRALIA
2 | CANADA
3 | CHINA
4 | DENMARK
5 | FRANCE
6 | HONG KONG
7 | ICELAND
8 | ITALY
9 | JAPAN
10 | KOREA
11 | NETHERLANDS
12 | NEW ZEALAND
13 | NORWAY
14 | ROMANIA
15 | RUSSIA
16 | PORTUGAL
17 | SOUTH AFRICA
18 | SWITZERLAND
19 | TAIWAN
20 | UNITED KINGDOM
21 | UNITED STATES OF AMERICA

## Slide 18
ASR reported locations around the globe

## Slide 19: ASR
ASR is the most common form of alkali-aggregate reaction (AAR) in concrete; the other, much less common, form is alkali-carbonate reaction (ACR).
For damaging reaction to take place the following need to be present in sufficient quantities.
High alkali cement
Reactive aggregate
Moisture [above 75%RH within the concrete]

## Slide 20: ASR
Aggregate reactivity depends directly on the alkalinity (typically expressed as pH) of the solution in the concrete pores. This alkalinity generally primarily reflects the level of water-soluble alkalis (sodium and potassium) in the concrete. These alkalis are typically derived from the Portland cement.

## Slide 21: Chemistry of Alkali Silica Reaction
Cement production involves raw materials that contain alkalis in the range of 0.2 to 1.5 percent of Na2O
This generates a pore fluid with high pH (12.5 to 13.5)
Strong alkalinity causes the acidic siliceous material to react

## Slide 22: ASTM specification
ASTM C150 designates cements with more than 0.6 percent of Na2O as high-alkali cements
Even with low alkali content, but sufficient amount of cement, alkali-silica reactions can occur
Investigations show that if total alkali content is less than 3 kg/m3, alkali-silica reactions will not occur (ASTM 1293, 1.25% alkali of 420kg/m3 =5.25kg/m3)

## Slide 23: Other sources of alkali
Even if alkali content is small, there is a chance of alkali-silica reaction due to
  alkaline admixtures
  aggregates that are contaminated
  penetration of seawater
  deicing solutions

## Slide 24
Reactive Silica
Silica tetrahedron:
Amorphous Silica
Crystalline Silica
Creation of alkali-silica gel

## Slide 25
Reactive Silica
Creation of alkali-silica gel
Amorphous or disordered silica = most chemically reactive
Common reactive minerals:
strained quartz
opal
obsidian
cristobalite
tridymite
chelcedony
cherts
cryptocrystalline volcanic rocks

## Slide 26
1. Siliceous aggregate in solution
Creation of alkali-silica gel

## Slide 27
2. Surface of aggregate is attacked by OH-
H20 + Si-O-Si
Si-OH…OH-Si
Creation of alkali-silica gel

## Slide 28
3. Silanol groups (Si-OH) on surface are broken
down by OH- into SiO- molecules
Si-OH + OH-
SiO- + H20
Creation of alkali-silica gel

## Slide 29
4. Released SiO- molecules attract alkali cations in pore solution, forming an alkali-silica gel around the aggregate.
Creation of alkali-silica gel
Si-OH + Na+ + OH-
Si-O-Na + H20

## Slide 30
5. Alkali-silica gel takes in water, expanding and exerting an osmotic pressure against the surrounding paste or aggregate.
Creation of alkali-silica gel

## Slide 31
6. When the expansionary pressure exceeds the tensile strength of the concrete, the concrete cracks.
Creation of alkali-silica gel

## Slide 32
7. When cracks reach the surface of a structure, “map cracking” results. Other symptoms of ASR damage includes the presence of gel and staining.
Creation of alkali-silica gel

## Slide 33
8. Once ASR damage has begun:
Creation of alkali-silica gel
Expansion and cracking of concrete
Increased permeability
More water and external alkalis penetrate concrete
Increased ASR damage

## Slide 34
Images of ASR damage

## Slide 35: SILICA MINERALS IN ORDER OF DECREASING REACTIVITY
# Amorphous silica: sedimentary or volcanic glass (a volcanic glass that is devitrified and/or mostly recrystallized may still be reactive)
# Opal
# Unstable crystalline silica (tridymite and cristobalite)
# Chert
# Chalcedony
# Other cryptocrystalline forms of silica
# Metamorphically granulated and distorted quartz
# Stressed quartz
# Imperfectly crystallized quartz
# Pure quartz occurring in perfect crystals

## Slide 36: ROCKS IN ORDER OF DECREASING REACTIVITY
# Volcanic glasses, including tuffs (especially highly siliceous ones)
# Metaquartzites metamorphosed sandstones)
# Highly granulated granite gneisses
# Highly stressed granite gneisses
# Other silica-bearing metamorphic rocks
# Siliceous and micaceous schists and phyllites
# Well-crystallized igneous rock
# Pegmatitic (coarsely crystallized) igneous rock
# Nonsiliceous rock

## Slide 37
ASR Research Time Line

## Slide 38
1. Stanton, 1940, California Division of Highway
2. Mather, 1941, Concrete Laboratory of the Corps of Engineers
3. ASTM C 227-10, 1950, Standard Test Method for Potential Alkali Reactivity of Cement-Aggregate Combinations
4. ASTM C 289, Quick chemical method, 1952
1940-1960
5. The Conrow test, 1952, ASTM C 342, 1954- withdrawn -2001
7. ASTM C1293, Concrete Prism Test, 1950s, Swenson and Gillott,
8. Gel pat test, Jones and Tarleton, 1958
6. ASTM C 295, Petrographic Examination of Aggregates, 1954

## Slide 39
9. ROCK CYLINDER METHOD, 1966
10. Nordtest accelerated alkali-silica reactivity test, Saturated NaCl bath method Chatterji , 1978
11. JIS A1146, Mortar bar test method, Japanese Industrial Standard (JIS)
12. Accelerated Danish mortar bar test, Jensen 1982
13. Evaluation of the state of alkali-silica reactivity in hardened concrete, Stark, 1985
14. ASTM C 1260, Accelerated mortar bar test (AMBT); South African mortar-bar test- Oberholster and Davies, 1986,
15. Uranyl acetate gel fluorescence test, Natesaiyer and Hover, 1988
1960 -1990

## Slide 40
1991 -2010
16. Autoclave mortar bar test, Fournier et al. (1991)
18. Modified gel pat test, Fournier, 1993
19. Chinese concrete microbar test (RILEM AAR-5)
20. Chinese autoclave test (CES 48:93), Japanese autoclave test, JIS A 1804
23. Modified versions of ASTM C 1260 and ASTM C 1293,Gress, 2001
17. Accelerated concrete prism test, Ranc and Debray, 1992
21. Chinese accelerated mortar bar method—CAMBT, 1998
22. Chinese concrete microbar test (RILEM AAR-5), 1999
24. Universal accelerated test for alkali-silica and alkali-carbonate reactivity of concrete aggregates, modified CAMBT, Duyou et al., 2008

## Slide 41
Common Test Methods to assess ASR

## Slide 42
RILEM SURVEY (Nixon And Sims 1996)
Reunion Internationale des Laboratoires et Experts des Materiaux, Systemes de Construction et Ouvrages (French: International Union of Laboratories and Experts in Construction Materials, Systems, and Structures)

## Slide 43
All countries, reported that no one test is capable of providing a comprehensive assessment of aggregates for their alkali-aggregate reactivity.

## Slide 44
Part 2:
Introduction to MCPT

## Slide 45: Introduction to MCPT
MCPT has been developed to determine aggregate reactivity, with:
- Similar reliability as ASTM C 1293 test but shorter test duration
(56 days vs. 1 year)
- Less aggressive exposure conditions than ASTM C 1260 test but better reliability

## Slide 46: Variables
Variable test conditions
  Storage environment
    Exposure condition
      1N NaOH
      100% RH
      100% RH (Towel Wrapped)
    Temperature
      38 C
      60 C
      80 C
  Sample Shape
    Prism (2” x 2” x 11.25”)
    Cylinder (2” dia x 11.25” long)
  Soak Solution Alkalinity (0.5N, 1.0N, and 1.5N NaOH solutions)

## Slide 47: Aggregates used in the Variables
Four known different reactive aggregates were used for these variables. These are as follows:
  Spratt Limestone of Ontario, Canada,
  New Mexico, Las Placitas-Rhyolite,
  North Carolina, Gold Hill -Argillite,
  South Dakota, Dell Rapids – Quartzite

## Slide 48
Effect of Storage Condition
1N NaOH Soak Solution
100% RH, Towel Wrapped
100% RH, Free standing

## Slide 49: Effect of Storage Condition on Expansion in MCPT
Chart: SP- MCPT Expansion with Different Curing Conditions
| 0 | 3 | 7 | 10 | 14 | 21 | 28 | 42 | 56 | 70 | 84
L4-SP-1N NaOH | 0 | 0.007 | 0.028667 | 0.049 | 0.067667 | 0.094 | 0.11233 | 0.13333 | 0.149 | 0.16367 | 0.17933
L7-SP-Towel Wrap | 0 | 0.009 | 0.015667 | 0.029667 | 0.041333 | 0.055333 | 0.07 | 0.087667 | 0.093 | 0.096333 | 0.098
L6-SP-Free Standing | 0 | 0.013 | 0.015 | 0.0255 | 0.039 | 0.058 | 0.067 | 0.082 | 0.09 | 0.0935 | 0.097

## Slide 50: Soak Solution Alkalinity (0.5N, 1.0N, and 1.5N NaOH solutions)
Chart: Alkali Solution Variability in MCPT
| 0 | 3 | 7 | 10 | 14 | 21 | 28 | 42 | 56 | 70 | 84
L4-SP_1 N NaOH | 0 | 0.007 | 0.028667 | 0.049 | 0.067667 | 0.094 | 0.11233 | 0.13333 | 0.149 | 0.16367 | 0.17933
L30-SP_1.5 N NaOH | 0 | 0.013667 | 0.026667 | 0.041667 | 0.063 | 0.096963 | 0.12667 | 0.163 | 0.18967 | 0.20667 | 0.22467
L31-SP_0.5 N NaOH | 0 | 0.004 | 0.0093333 | 0.017333 | 0.028889 | 0.055333 | 0.069 | 0.092667 | 0.111 | 0.11767 | 0.12433

## Slide 51
Prisms vs. Cylinders

## Slide 52: Effect of Sample Shape on Expansion in MCPT Spratt Limestone
Chart: SP- Miniature Concrete Prism vs Concrete Cylinder Expansion
| 0 | 3 | 7 | 10 | 14 | 21 | 28 | 42 | 56 | 70 | 84
L4-SP-Prism | 0 | 0.007 | 0.028667 | 0.049 | 0.067667 | 0.094 | 0.11233 | 0.13333 | 0.149 | 0.16367 | 0.17933
L14-SP-Cyln | 0 | 0.0083333 | 0.028333 | 0.048333 | 0.079333 | 0.12067 | 0.14733 | 0.18067 | 0.197 | 0.21667 | 0.24667

## Slide 53: Effect of Temperature on Expansion in MCPT Spratt Limestone
Chart: SP- Miniature Concrete Prism Expansion with Different Temperatures
| 0 | 3 | 7 | 10 | 14 | 21 | 28 | 42 | 56 | 70 | 84
L4-SP-60C | 0 | 0.007 | 0.028667 | 0.049 | 0.067667 | 0.094 | 0.11233 | 0.13333 | 0.149 | 0.16367 | 0.17933
L10-SP-38C | 0 | 0.001 | 0.003 | 0.004 | 0.0045 | 0.0105 | 0.0175 | 0.034 | 0.0545 | 0.0735 | 0.085853
L20-SP-80C | 0 | 0.015 | 0.040333 | 0.054333 | 0.073 | 0.10033 | 0.12833 | 0.17467 | 0.21533 | 0.268 | 0.31533

## Slide 54: MCPT Method Parameters
Mixture Proportions and Specimen Dimensions
  Specimen size = 2 in. x 2 in. x 11.25 in.
  Max. Size of Aggregate = ½ in. (12.5 mm)
  Volume Fraction of = 0.65
  Dry Rodded Coarse Aggregate
  in Unit Volume of Concrete
  Coarse Aggregate Grading Requirement:
Sieve Size, mm |  | Mass, %
Passing | Retained | 
12.5 | 9.5 | 57.5
9.5 | 4.75 | 42.5

## Slide 55: MCPT Method (continued)
Test Procedure
  Cement Content (same as C1293) = 420 kg/m3
  Cement Alkali Content = 0.9% ± 0.1% Na2Oeq.
  Alkali Boost, (Total Alkali Content) = 1.25% Na2Oeq. by mass of cement
  Water-to-cement ratio = 0.45
  Storage Environment = 1N NaOH Solution
  Storage Temperature = 60⁰C
  Initial Pass/Fail Criteria = Exp. limit of 0.04% at 56 days
  Use non-reactive fine aggregate, when evaluating coarse aggregate
  Use non-reactive coarse aggregate, when evaluating fine aggregate
  Specimens are cured in 60⁰C water for 1 day after demolding
  before the specimens are immersed in 1N NaOH solution.

## Slide 56: Expansion Data of Test Specimens Containing Selected Aggregates in Different Test Methods (Note: red:- reactive, green:- non-reactive)
Aggregate Identity | % Expansion |  | 
 | MCPT, 56 Days | ASTM C 1293, 365 days | ASTM C 1260, 14 days
L4-SP | 0.149 | 0.181 | 0.350
L11-SD | 0.099 | 0.109 | 0.220
L15-NM | 0.185 | 0.251 | 0.900
L19-NC | 0.149 | 0.192 | 0.530
L23-BB | 0.017 | 0.032 | 0.042
L54-Galena-IL | 0.046 | 0.050 | 0.235
L32-QP | 0.070 | 0.070 | 0.080*
L34-SLC | 0.039 | 0.030 | 0.190**
L59-MSP | 0.023 | 0.030 | 0.100**
L56-TX | 0.440 | 0.590 | 0.640
L35-GI | 0.091 | 0.090 | 0.260
L36-SB | 0.115 | 0.150 | 0.460

## Slide 57: Proposed criteria for characterizing aggregate reactivity in MCPT protocol
Degree of Reactivity | % Expansion at 56 Days | Rate of Expansion from 8 to 10 weeks
Non-reactive | < 0.040 % | < 0.010% per two weeks
Low | 0.035% – 0.060% | > 0.010% per two weeks
Moderate | 0.060% – 0.120% | N/A
High | > 0.120% | N/A

## Slide 58: Comparison of MCPT-56 with CPT-365
Chart: ASTM C 1293, CPT vs. MCPT 56 Days Expansion
| 0.18500000000000016 | 0.14900000000000016 | 0.14900000000000016 | 9.9500000000000144E-2 | 2.0000000000000011E-2 | 4.5999999999999999E-2 | 7.0000000000000021E-2 | 3.9000000000000014E-2 | 2.3299999999999998E-2 | 0.44 | 9.1000000000000025E-2 | 0.115
 | 0.251 | 0.181 | 0.192 | 0.109 | 0.03 | 0.05 | 0.07 | 0.03 | 0.03 | 0.59 | 0.09 | 0.15
MCPT
0.04% limit at 56 days
CPT
0.04% limit at 365 days

## Slide 59
Part 3: Evaluation of Effectiveness of SCMs for ASR Mitigation in the MCPT

## Slide 60: Supplementary Cementing Materials (SCMs)

## Slide 61: Fly Ashes for ASR Mitigation in the MCPT
Three fly ashes
  Low-lime fly ash
  intermediate-lime fly ash, and
  high-lime fly ash
All were used at a dosage of 25% by mass replacement of cement

## Slide 62: Effectiveness of low-lime, intermediate-lime and high-lime fly ashes in mitigating ASR in MCPT method using Spratt limestone as reactive aggregate

## Slide 63
Later nine different fly ashes (3 high-lime -HL, 3 low-lime-LL and 3 intermediate-lime- IL fly ashes) at 25% cement replacement levels were investigated

## Slide 64: Nine different fly ashes (3 high-lime, 3 low-lime and 3 intermediate-lime fly ashes) at 25% cement replacement levels

## Slide 65: Effectiveness of Slag, Meta-kaolin, Silica fume and LiNO3 in mitigating ASR
Spratt limestone as reactive aggregate
Mass replacement of cement
Slag was used at a dosage of 40%
Metakaolin was used at a dosage of 10%
Silica Fume was used at a dosage of 10%
Additionally LiNO3 was used at a dosage of 100%

## Slide 66: Effectiveness of Slag, Meta-kaolin, Silica fume and LiNO3 in mitigating ASR in MCPT method using Spratt limestone as reactive aggregate

## Slide 67
Part 3: Effect of Prolonged Curing of Test Specimens on the Performance of Fly Ashes in MCPT Test Method

## Slide 68: Effect of Prolonged Curing of Test Specimens on the Performance of Fly Ashes in MCPT Test Method
MCPT test specimens cured for varying lengths of time Days:
1 day, 7 days, 14 days and 28 days ; before they were exposed to 1N NaOH solution
Three fly ashes of significantly different chemical composition (Low-lime fly ash, intermediate-lime fly ash and high-lime fly ash) were selected.

## Slide 69: Low Lime-Class F fly ash at 25% cement replacement

## Slide 70: Intermediate Lime fly ash at 25% cement replacement

## Slide 71: High Lime-Class C fly ash at 25% cement replacement

## Slide 72: Conclusions
The findings from the extended initial curing of test specimens in MCPT showed that there is no added benefit in increasing the duration of initial curing in assessing the effectiveness of ASR mitigation measures such as supplementary cementitious materials.
Based on the results, MCPT appears to be a viable test method that can potentially replace both AMBT (ASTM C 1260) and CPT (ASTM C 1293) for routine ASR-related testing.

## Slide 73: Future Steps
Develop a protocol for evaluation of Job Mixtures for Potential ASR

## Slide 74: Questions?
elatife@clemson.edu