## Slide 1: Investigation of ASR expansion due to total alkali and internal alkali (concentration) in the concrete
E. R. Latifee, PhD
10th Global Engineering, Science and Technology Conference
January 2, 2015, BIAM Foundation,
63 Eskaton, Dhaka, Bangladesh

## Slide 2: Acknowledgement
Dr. Prasad Rangaraju, Clemson University, U.S.A.
Dr. Paul Virmani, FHWA,U.S.A.

## Slide 3: ASR - Alkali Silica Reaction
Alkalis
+
Reactive Silica
+
Moisture
ASR Gel which expands
Concrete expansion and
cracking
What is Alkali Silica Reaction?
Alkali-silica reaction (ASR) is a heterogeneous chemical reaction between alkali ions (Na+ and K+) and hydroxide ions (OH-) in the concrete pore solution, generally derived from the Portland cement, and forms of reactive silica (SiO2) in the aggregate (eg: chert, quartzite, opal, strained quartz crystals).

## Slide 4
Creation of alkali-silica gel and cracking of concrete

## Slide 5: SEM and EDX Analysis of Spratt Specimen
scanning electron microscope Image
Energy-dispersive X-ray spectroscopy

## Slide 6: Alkali-Silica Reaction Distresses in the field
Notes: Delete

## Slide 7: MCPT Samples

## Slide 8: Materials

## Slide 9: Reference bar and MCPT specimen reading in the comparator

## Slide 10
Storage Condition
1N NaOH Soak Solution
10
60 deg. C Storage Room

## Slide 11
Cement alkali of 0.82% boosted to 1.25% Na2Oeq and 1 N NaOHCement soak solution matching pore solution
Cement alkali of 0.82% Na2Oeq and 0.7 N NaOH soak solution matching pore solution
Cement alkali of 0.49% Na2Oeq and 0.45 N NaOH soak solution matching pore solution
The pore solution composition of the concrete mixtures was predicted based on the equation
[OH-] = 0.339 Na2Oeq%/(w/c) + 0.022 +/- 0.06 mol/L
-Stark and Diamond (1993)
Different Alkali Cements and Soak-solutions- Internal/Pore solution

## Slide 12
Expansion curves of different cement alkalinity and soak solution alkalinity concrete prisms in the MCPT

## Slide 13
Figure: 28-day % expansion vs. Soak solution alkalinity
Figure: 56-day % expansion vs. Soak solution alkalinity

## Slide 14
Alkali loading of different MCPT specimens
Alkali loading, kg/m3 (lb/yd3) = Cement content, kg/m3 (lb/yd3) x Cement Alkalinity (Na2Oeq %).

## Slide 15
Alkali loading and corresponding 56-day expansions of MCPT specimens

## Slide 16
Comparison between alkali loading(lb/yd3) &
56-day % expansion

## Slide 17
Comparison between alkali loading(kg/m3) &
56-day % expansion

## Slide 18: Implementation of MCPT Method and AASHTO Code
Round Robin Testing of MCPT -conducted across six labs:
  Nebraska DOT( Department of Transportation)
  Delaware DOT
  Turner-Fairbanks Highway Research Center, FHWA
  Purdue University
  Bowser Morner, Inc.
  Clemson University
AASHTO adopted Miniature Concrete Prism Test as a provisional test standard AASHTO TP 111 in 2014.
Questions?
ERLATIFEE@GMAIL.COM